E-GUN standard process user manual

Existing processes

Creation date: 04/2008

Revision date: 04/2008

Latest revision date: 05/2024

| Evaporation metals | Ti, Al, Ni |
| --- | --- |
| Base pressure | 3E-6 |
| Evaporation time | 1 hour |
| Evaporation speed | 3A/sec |
| Evaporation power | 20~40%(Emission power) |
| Evaporation thickness | Ti, Al < 7.5kA, Ni< 1kA |
| Resistance of metal sheet | 74.6m ohm |