CF-C05 - standard process for 6” chemical wet etching workstation

| Cleaning Station parts. SC-1; SC-2; DHF; SPM. Types of chemicals; NH4OH : H2O2 : H2O; HCl : H2O2 : H2O; HF : H2O; H2SO4 : H2O2. Process concentration; 1 : 4 : 20; 1 : 1 : 6; 1 : 50; 4 : 1. Process temperature; 75°C; 75°C; 22°C; 120°C. Process time; 600sec; 600sec; 60sec; 600sec. Purpose of chemicals; Remove particles/organic pollutants; Remove metal pollutants; Remove native oxide layer; Remove organic pollutants. Photoresist Station/Wet Etching Station parts. Wafer P.R. Strip (on non-metal); Mask P.R. Strip Mask Clean; B.O.E. 7:1; H3PO4. Types of chemicals; H2SO4 : H2O2; H2SO4 : H2O2; B.O.E. 7:1 (NH4F:HF); H3PO4. Process concentration; Pure H2SO4 + 100 ml H2O2; Pure H2SO4 + 100 ml H2O2; Pure B.O.E.; H3PO4+ H2O 200 ml. Process temperature; 120°C; 105°C; Ambient temperature; 150°C. Process time; 600sec; 600sec; Depends on required etching thickness; Depends on required etching thickness. Purpose of chemicals; Remove organic pollutants; Remove organic pollutants Clean photomask dirt; Etch silicon dioxide; Remove Si3N4. |  |  |  |
| --- | --- | --- | --- |

Process conditions currently open

Cleaning Station

- Before long gate oxide layer/before manufacturing structures directly related to electricity/forming film thicknesses less than 100Å

RCA Clean: SPM → QDR → DHF → QDR → SC-1 → QDR → SC-2 → QDR → DHF → QDR → SPIN DRY

- Cleaning before general high-temperature and high vacuum processes/forming film thicknesses less than 100Å

STD Clean: SC-1 → QDR → SC-2 → QDR → SPIN DRY

- Cleaning before general high-temperature and high vacuum processes, but worried about the effect of native oxide layer

STD + DHF dip Clean: SC-1 → QDR → SC-2 → QDR → DHF → QDR → SPIN DRY

- After etching/cleaning after non-metal chemical mechanical polishing/removing side wall polymer

SC-1 → QDR → SPIN DRY

- Only when removing native oxide layer

DHF → QDR → SPIN DRY

- Cleaning before Poly Silicon TFT process gate oxide

SPM → QDR → DHF → QDR → SC-2 → QDR → DHF → QDR → SPIN DRY

Photoresist Station

- Removing front-end process photoresist

SPM#2 → QDR → SPIN DRY

- Cleaning photomask/removing photomask photoresist

SPM#1 → QDR → natural dry

Wet Etching station

- SiO2/TEOS wet etching of front-end process (can enter wafers with photoresist patterns)

B.O.E. 7:1 → QDR → SPIN DRY

- Removing front-end process silicon nitride (Si3N4) film

H3PO4 → QDR → SPIN DRY