Wet Bench (Class 100) Etching Workstation CF-C05

Knowledge Evaluation Form

- Wearing of Protective Gear

- Please explain how to wear or remove protective gear in sequence. 	□

- How to clean protective gear after use: Please explain the acid- and alkali-resistant gloves, apron, and safety mask separately.	□

- Awareness of Equipment Hazards and Crisis Management

- Hazards of chemicals used in each process tank	□

- For SC-1 and SC-2 tanks, how low should the temperature be before discharging chemicals? How should temperature reduction and chemical discharge proceed? 	□

- For SPM tank, SPM #1, and SPM #2 tanks (sulfuric acid tank), how low should the temperature be before discharging chemicals? How should temperature reduction and chemical discharge proceed? 	□

- Methods to stop the machine in emergency situations	□

- What is the purpose of the Material Safety Data Sheet (MSDS)? What is the purpose of the litmus paper? 	□

- Location and method of use of the shower and eyewash station? 	□

- Method of use of hexafluorine and diphoterine? 	□

- Method of use and usage timing of calcium gluconate? 	□

- Where should chemical waste (airlaid papers) used at this station be disposed?

- Are the chemicals used at this station organic or inorganic?

- Relevant Regulations on Pollution Control at the Equipment-end and Pollution Control Principles at Process-end

- Please explain with regards to the Cleaning Station, what materials are restricted from this equipment? 	□

- Please explain with regards to the Photoresist Station, what materials are restricted from this equipment? 	□

- Please explain with regards to the Etching Station, what materials are restricted from this equipment? 	□

- Cassette confirmation at the furnace pre-cleaning station and cleanliness guidelines for the spin dryer	□

- Cassette confirmation at the photoresist station and wet etching station, and cleanliness guidelines of the spin dryer	□

- Cleanliness level classification of cassette handle at cleaning station/photoresist station	□

- Cleanliness level classification of cassette handle at wet etching station/metal station	□

- Before using the sulfuric acid tank in the photoresist station, which front-end process should the wafer go thru? Why? 	□

- Basic operational knowledge of each chemical tank, operational procedures for chemical replacement and preparation, principles and operational procedures of wet cleaning and etching

- Which processes are suited for SC-1? What are its action principles for pollution removal? 	□

- What is the process concentration, process temperature, process time and replacement timing for SC-1? How to replace? (hands-on demonstration)	□

- Which processes are suited for SC-2? What are its action principles for pollution removal? 	□

- What is the process concentration, temperature, time and replacement timing for SC-2? How to replace? (hands-on demonstration)	□

- Which processes are suited for DHF? What are its action principles for chemical reactions? 	□

- What is the process concentration, temperature, time and replacement timing for DHF? How to replace? (hands-on demonstration)	□

- Which processes are suited for SPM sulfuric acid tank? What are its action principles for pollution removal? 	□

- What is the process concentration, temperature, time and replacement timing for SPM sulfuric acid tank? How to replace? (hands-on demonstration)	□

- Which processes are suited for B.O.E.7:1? What are its action principles for thin film removal? 	□

- What is the process temperature, time and replacement timing for B.O.E.7:1 solution? How to replace? (hands-on demonstration)	□

- Which processes are suited for H3PO4 solution? What are its action principles for thin film removal? 	□

- What is the process concentration, temperature, time and replacement timing for H3PO4 solution? How to replace? (hands-on demonstration)	□

- Which processes are suited for SPM #2 sulfuric acid tank? What are its action principles for pollution removal? 	□

- What is the process concentration, temperature, time and replacement timing for SPM #2 sulfuric acid tank? How to replace? (hands-on demonstration)	□

- Is photoresist removal from photomask or photomask cleaning open to self-operation by users? 	□

- Can photoresist removal from photomask and general photoresist removal share the same sulfuric acid tank? Why? 	□

- Can photoresist removal from metal layer be carried out through the photoresist removal process by soaking in sulfuric acid solution? Why? 	□

- Can DHF solution be filled into a glass or quartz tank? Why? 	□

- What is the wet etching process? What are the pros and cons compared to the dry etching process? 	□

- Why add 200 ml of H2O when the temperature is 120°C when preparing the hot phosphoric acid solution? 	□

- Why refill with H2O2 when carrying out the SC-1, SC-2, and SPM processes? 	□

- In the manufacturing of components, wafers need to go through the cleaning process before which processes? 	□

- What is the Piranha solution? Which contaminants are removed from the wafer? 	□

- Please explain the differences between hydrophilic and hydrophobic surfaces of wafers. 	□

- What are the differences in vacuum pen usage in the Wet Bench area? 	□

- Please explain etching selectivity. How do you test the etching rate of the B.O.E. solution or phosphoric acid solution?	□

- Please explain how the electrical properties of components will be affected by uncleaned particles or metal contaminants on wafer surfaces.	□

- Please explain how the electrical properties of components will be affected by uncleaned organic matter and native oxide layers on wafer surfaces.	□

- Please explain how the electrical properties of components will be affected as the roughness of wafer surfaces increases.	□

- Which instrument can be used to check the particle and metal contaminant contents on wafer surfaces after cleaning? 	□

- Which instrument can be used to check the roughness and organic contaminant contents on wafer surfaces after cleaning? 	□

- Basic Procedures for Each Standard Process

- RCA Clean process needs to be carried out before which process? 	□

- STD Clean process needs to be carried out before which process? 	□

- STD + HF dip Clean process needs to be carried out before which process? 	□

- Which process should be selected for Side Wall Polymer removal? 	□

- Which wafer cleaning method should be selected after Laser Mark? 	□

- Which wafer cleaning method should be selected after front-end CMP process? 	□

- Which wafer cleaning method should be selected before Metal PVD process? 	□

- Operational procedures for QDR tank

- In the cleaning process, the QDR method is normally used for cleaning wafers. What is QDR? 	□

- What is the purpose of QDR in the wet wafer cleaning process? 	□

- What is deionized water in the wet wafer cleaning process? What is the resistivity of pure water, DI Water at 25°C? 	□

- Carry out a wafer cleaning process (hands-on demonstration)	□

- How to select recipe to change the number of cleaning times for QDR tank (hands-on demonstration)	□

- Operational procedures for Spin dryer

- How to execute wafer drying process at the TSRI? 	□

- Explain the action principles of drying the wafer with the spin dryer and explain the purpose of the static elimination installation	□

- Explain the usage timing of Rinse Mode and Dry Mode	□

- Operational procedures for Spin dryer (hands-on demonstration) 	□

- Usage and handling of various chemicals at the equipment-end

- Please explain relevant regulations on placement and use of small-package chemicals in the Class 100 clean room	□

- Can chemicals be prepared with the beaker or petri dish at the WET BENCH of TSRI? Why? 	□

- Where should chemicals be prepared and heated with a hot plate at TSRI? 	□

- Inspection of machine before and after use

- How do you identify a process as front-end or back-end at TSRI? 	□

- Before using the equipment, check the equipment status at the equipment-end and process-end	□

- Explain the time segments during which the equipment can be reserved and used	□

- Record needs to be logged and checked after completing equipment use	□