Wet Bench Front-end Chemical Wet Etching Workstation (CF-C10)

Knowledge Evaluation Form

- Inspection of equipment before and after use

  - How do you identify a process as front-end or back-end at TSRI?

  - Checking the condition of the equipment at the equipment-end and process-end before using it

  - Explaining the time slots when the equipment can be reserved and used

  - Registration and checks required after completing the use of the equipment

- Awareness of Equipment Hazards and Crisis Management

  - Hazards of chemicals used in each process tank

  - Notes on the operation of the robotic arm

  - How to stop the machine in emergency situations

  - Purpose of the Material Safety Data Sheet (MSDS)? What is the purpose of the litmus paper?

  - Troubleshooting and reset of the equipment after a process-end alarm

  - Location and method of use of the shower and eyewash station?

  - Method of use of hexafluorine and diphoterine?

  - Method of use and usage timing of calcium gluconate?

  - Are the chemicals used at this station organic or inorganic?

- Relevant Regulations on Pollution Control at the Equipment-end and Pollution Control Principles at Process-end

  - Selection and checking of cassettes at the cleaning station and the guidelines for cleanliness control of the spin dryer

  - Selection and checking of cassettes at the photoresist/wet etching station and the guidelines for cleanliness control of the spin dryer

  - Before using the sulfuric acid tank in the photoresist station, which front-end process should the wafer go thru? Why?

  - Please explain with regards to the Cleaning Station, what materials are restricted from this equipment?

  - Please explain, with regards to the photoresist and wet etching stations, what materials are restricted from this equipment?

  - Please explain with regards to the Etching Station, what materials are restricted from this equipment?

- Basic operational knowledge of each chemical tank, operational procedures for chemical replacement and preparation, principles and operational procedures of wet cleaning and etching

  - Which processes are suited for SC-1? What are its action principles for pollution removal?

  - What are the soaking concentration, process temperature, process time and timing of replacement for SC-1? How to replace? (hands-on demonstration)

  - Which processes are suited for SC-2? What are its action principles for pollution removal?

  - What are the soaking concentration, process temperature, process time and timing of replacement for SC-2? How to replace? (hands-on demonstration)

  - Which processes are suited for DHF? What are its action principles for chemical reactions?

  - What are the soaking concentration, process temperature, process time and timing of replacement for DHF? How to replace? (hands-on demonstration)

  - Which processes are suited for SPM (1) sulfuric acid tank? What are its action principles for pollution removal?

  - What are the soaking concentration, process temperature, process time and timing of replacement for SPM (1) sulfuric acid tank? How to replace? (hands-on demonstration)

  - Which processes are suited for B.O.E.7:1? What are its action principles for thin film removal?

  - What are the process temperature, process time and timing of replacement for B.O.E.7:1 solutions? How to replace? (hands-on demonstration)

  - Which processes are suited for H3PO4 solution? What are its action principles for thin film removal?

  - What are the process temperature, process time and timing of replacement for H3PO4 tanks? How to replace? (hands-on demonstration)

  - Which processes are suited for SPM #2 sulfuric acid tank? What are its action principles for pollution removal?

  - What are the process concentration, temperature, time and timing of replacement for SPM (2) sulfuric acid tank? How to replace? (hands-on demonstration)

  - What is the wet etching process? What are the pros and cons compared to the dry etching process?

  - Why add 200 ml of H2O when the temperature is 120°C when preparing the hot phosphoric acid solution?

  - Why refill with H2O2 when carrying out the SC-1, SC-2, and SPM processes?

  - In the manufacturing of components, wafers need to go through the cleaning process before which processes?

  - What is the Piranha mixture? Which contaminants are removed from the wafer?

  - Please explain the differences between hydrophilic and hydrophobic surfaces of wafers.

  - What are the differences in vacuum pen usage in the Wet Bench area?

  - Please explain etching selectivity. How to test the etching rate of the B.O.E. solution or phosphoric acid solution?

- The Methods for Testing of Contaminants after Wafer Cleaning and the Effects on Electrical Properties

  - Please explain how the electrical properties of components will be affected by uncleaned particles or metal contaminants on wafer surfaces.

  - Please explain how the electrical properties of components will be affected by uncleaned organic matters or native oxide layers on wafer surfaces.

  - Please explain how the electrical properties of components will be affected as the roughness of wafer surfaces become greater.

  - Which instrument can be used to check the particle and metal contaminant contents on wafer surfaces after cleaning?

  - Which instrument can be used to check the roughness and organic contaminant contents on wafer surfaces after cleaning?

- Basic Procedures for Each Standard Process

  - RCA Clean process needs to be carried out before which process?

  - STD Clean process needs to be carried out before which process?

  - STD + HF dip Clean process needs to be carried out before which process?

  - Which process should be selected for Side Wall Polymer removal?

  - Which wafer cleaning method should be selected after Laser Mark?

  - Which wafer cleaning method should be selected after front-end CMP process?

  - Which wafer cleaning method should be selected before Metal PVD process?

- Operational Procedures and Use of QDR Tank?

  - In the cleaning process, the QDR method is normally used for cleaning wafers. What is QDR?

  - What is the purpose of QDR in the wet wafer cleaning process?

  - What is deionized water in the wet wafer cleaning process? What is the resistivity of (pure water, DI Water) at 25°C?

  - Performing a single wafer cleaning process (hands-on demonstration)

  - How to change the number of rinses of the QDR tank during an automatic process? (hands-on demonstration)

- Operational procedures for Spin dryer

  - How to execute wafer drying process at the TSRI?

  - What are the principles of drying the wafer with a spin dryer, and what is the purpose of a static eliminator?

  - Explain the timing of use of the Rinse Mode and Dry Mode

  - Operational procedures for a spin dryer? (hands-on demonstration)

- Usage and handling of various chemicals at the equipment-end

  - Please explain the relevant requirements for the placement and use of small-package chemicals in the Class 100 Clean Room

  - Can chemicals be prepared with a beaker or petri dish at the Wet Bench of TSRI? Why?

  - Where should chemicals be prepared and then heated with a hot plate at TSRI?