AMAT Mirra Mesa

8-inch CMP - Standard Operating Procedures

- Check equipment condition (check the alarm messages of the equipment)

- Swipe the card to start up the machine.

- Distribute slurry into the slurry delivery system (SDS) and switch to the chemical delivery system (CDS) mode for Si or SiO2/SiN.

--See “SOP for Switching to Mega Chemical Tank”—

TSRI

- Pause the wet idle mode process:  STOP  Close

- Press Unload and insert the cassette.

- Scan the cassette and select a program.

  - Edit new if polishing is required, and edit disable otherwise.

(Pad 1 is used for Si polishing; Pad 2 is used for SiO2/Si3N4 polishing)

  - Select a Pad Conditioner program: “Dummy Condition” is generally used.

  - Select a polishing program (newly created program)

  - OK

- Start Processing  OK

References
1. AMAT (Applied Materials, Inc.)
https://www.appliedmaterials.com/zh-hant/products/mirra-mesa-cmp-200mm

2. E-Dot Technology Inc.

http://www.e-dot.com.tw/web/front/bin/home.phtml