Introduction of Focused Ion Beam/Electron Beam Dual Beam System

| Electron beam specifications |  |
| --- | --- |
| Resolving power | 2nm @ 15kV SE 5nm @ 1kV SE |
| Accelerating voltage | (SEM) 1~30kV |
| Electron emission source | Thermal Field emission |
| Range of magnification for observation | (SEM) 55x to 500kx |
| Ion beam specifications |  |
| Resolving power | 7nm guaranteed 5nm achievable |
| Accelerating voltage | (FIB) 2~30 kV |
| Ion emission source | Type: Gallium liquid metal Life time:1000 hours |
| Stability of position of ion beam irradiation | Beam shift spec.: mechanically <5μm, electrically 0.1% |
| Specifications of movable stage |  |
| Direction axis | At least 5-axis motorized |
| Specifications of movement X, Y | Repeatability 1 μm, at 0 degrees tilt Repeatability 2 μm at 52 degrees tilt. Travel ≧± 75 mm |
| Z | ≧ 10mm |
| Rotation | 360o |
| Tilt | -3 o ~ 60 o |
| Sample stage | 150 mm + Stub holder |
| Applicable gases | Insulator Deposition Platinum Deposition Tungsten Deposition Selective Carbon Mill Insulator Enhanced Etch |
| Deposition power | Minimum deposited line width (ion beam, Pt): 100 nm Minimum deposited line width (e-beam, Pt) : 25 nm |
| Etching power | Minimum etched trench width (I-beam, Si): 30 nm (15 nm achieved ) |