8” fully automated surface profiler

Measurement

- Roughness

Profiling Performance

| - Scan Length: | 1μm to 5mm |
| --- | --- |
| - Scan Speed: | 2μm/s to 25mm/s |
| - Sampling Rate: | 5 to 2000Hz |
| - Vertical Range: | ±13μm / 0.0078Ǻ ±65μm / 0.0391Ǻ , ±327μm / 0.1953Ǻ |
| - Vertical Linearity: | 10Ǻ |
| - Horizontal Resolution | 0.1μm @ 1μm/s scan speed |
| - Maximum Sample Size: | 254 x 254mm |