Breakage Lines of I-line Stepper-Introduction

Chin-Tsai Hsu

Jan. 9, 2020

Instructions on Use of Breakage Lines of I-line Stepper

- Scope of exposure service for breakage lines

- Instructions on use of breakage lines

- Requirements on use of breakage lines

Scope of exposure service for breakage lines - (1)

Breakage line exposure can be divided into the following two processes:

Process 1: Exposure (zero layer) starts with a small breakage, followed by the subsequent process until the component is completed.

Process 2: Exposure (zero layer) starts with a whole breakage (6” or 8”), followed by a certain process, after which it is cut into a standard sized breakage, and then the process continues until the component is completed.

<Note>

- All breakages to be aligned for exposure must initially be cut into small breakages with a cutting machine.

- If the exposure procedures go through Process 2, their details must be discussed with the engineer.

Chin-Tsai Hsu ext.: 7648 cthsu@narlabs.org.tw

Scope of exposure service for breakage lines - (2)

Process for breakage line exposure

9-in-1 reticle

4-in-1 reticle

Breakage

start

start

Whole breakage

Cut into breakage after certain process

Note: Exposure of 2*2 dies is required for breakage alignment at a minimum

Pure I-line

WEPRINT/ELS7500

(using 4-in-1 reticle)

Mix-Match

(must be discussed with engineer!!)

1.2*1.2, 2*2, 2.5*2.5 cm2, 2”, 4”

(using standard, 9-in-1 or 4-in-1 reticle)

Mix-Match

Pure I-line

WEPRINT/ELS7500

2.5*2.5 cm2 (using 4-in-1 reticle)

4*4 cm2 (using standard reticle)

2*2, 2.5*2.5 cm2 (using 4-in-1 reticle)

(must be discussed with engineer!!)

Process for breakage line exposure

9-in-1 reticle

4-in-1 reticle

Breakage

start

start

Whole breakage

Cut into breakage after certain process

Note: Exposure of 2*2 dies is required for breakage alignment at a minimum

Pure I-line

WEPRINT/ELS7500

(using 4-in-1 reticle)

Mix-Match

(must be discussed with engineer!!)

1.2*1.2, 2*2, 2.5*2.5 cm2, 2”, 4”

(using standard, 9-in-1 or 4-in-1 reticle)

Mix-Match

Pure I-line

WEPRINT/ELS7500

2.5*2.5 cm2 (using 4-in-1 reticle)

4*4 cm2 (using standard reticle)

2*2, 2.5*2.5 cm2 (using 4-in-1 reticle)

(must be discussed with engineer!!)

Scope of exposure service for breakage lines - (3)

Process 1:

Subsequent process

Subsequent process

| Starting with small breakage of certain size |  | Component is completed |
| --- | --- | --- |

Scope of exposure service for breakage lines - (4)

| Process 2: Exposure (zero layer) starts with 6” or 8” | Whole breakage goes through subsequent process Whole breakage goes through subsequent process | Cut into small breakage after certain process |
| --- | --- | --- |

| Going through subsequent process with small breakage | Small breakage goes through subsequent process Small breakage goes through subsequent process | Component is completed <Note>Please discuss with the I-line engineer Chin-Tsai Hsu (ext. 7648) before exiting the breakage line process. |
| --- | --- | --- |

Instructions on use of breakage lines - (1)

The I-line Stepper is the primary machine for TSRI’s 6/8-inch exposure service. Although we have already provided the stage for breakage exposure service, we have to restrict the conditions for its use due to its non-standard exposure mode, which is likely to affect the primary 6/8-inch exposure service and the cleanliness of the machine.

OEM time: Tuesday and Thursday 14:00-16:00

Time for operation by yourself: Except during the office hours of 9:00-18:00 on Monday to Friday, you may use the machine.

Instructions on use of breakage lines - (2)

Thickness of breakage: must be 725 um.

Type: may be Si, compound semiconductors, glass, and LiTaO3 ceramic materials

Size:

25*25 mm2 breakage for standard OEM

Other sizes: 12*12, 20*20, 40*40mm2, 50*50mm2, 2”, 4”

<Note>

A breakage of the size of 12*12, 20*20 or 25*25mm 2 can be coated with photoresist and developed automatically in L09, while a breakage of any other size must be coated with photoresist and developed manually. For automatic photoresist coating and development of breakage in L09, contact Engineer Chao-Hsin Hung (ext. 7573). For manual photoresist coating, contact Engineer Hung-Chun Chen (ext. 7575).

Instructions on use of breakage lines - (3)

Reticle, exposure arrangement and size:

Range of reticle layout:

3.2 X 3.2mm2 (for 9 IN 1 reticle), 7.2 X 7.2 mm2 (for 4 IN 1 reticle)

Exposure arrangement and size:

5 X 5 map, stepping 4.5 X 4.5 mm2 (for 9 IN 1 reticle), 2 X 2 map, stepping 9 X 9 mm2 (for 4 IN 1 reticle)

- The unit above is the size on a wafer.

- For all-in-one reticles, contact Engineer Ying-Ling Hong (ext. 7746).

| 9 IN 1 reticle | 4 IN 1 reticle | 5x5 map (25mm2) 3.2x3.2 mm2 exposure area Stepping 4.5x4.5 mm2 | 2x2 map (25mm2) 7.2x7.2 mm2 exposure area Stepping 9x9 mm2 |
| --- | --- | --- | --- |

Instructions on use of breakage lines - (4)

Resolution and alignment error:

Resolution: single line 0.35 um/single hole 0.45 um

Alignment error: misalignment 1 um

| Minimum resolution: single line 0.35 um single hole 0.45 um |  | Reserve at least 1um for the design of layout alignment error |
| --- | --- | --- |

Instructions on use of breakage lines - (5)

Notes:

- Use a cutting machine to complete cutting breakages to be aligned.

- For non-standard wafer thickness, a dummy breakage is required (contact the engineer for more information).

- Mix-match exposure with other exposure tools is required (contact the engineers for more information).

- Exposure of special materials may be discussed with the engineer: cthsu@narlabs.org.tw (Chin-Tsai Hsu ext. 7648)

Requirements on use of breakage lines - (1)

<Notes>

A breakage must be cut flat, or the alignment service cannot be provided (except for single-layer exposure).

The back of a breakage must not be stained (e.g., marking, reverse permeation of photoresist...).

Photoresist coating on the edge of a breakage may be uneven or poorly covered, which may affect the quality near the edge.

The wafer must be cut flat, or the alignment service cannot be provided

A stained back of the wafer causes misalignment

The back of the wafer must have no markings; markings may cause defocus

The wafer must be cut flat, or the alignment service cannot be provided

A stained back of the wafer causes misalignment

The back of the wafer must have no markings; markings may cause defocus

|  |  |  | The corners of the back of the wafer are prone to having residual photoresists and need to be wiped clean with a dust-free cotton swab. |
| --- | --- | --- | --- |

Requirements on use of breakage lines - (2)

Process for breakage exposure:

| priming HMDS (L09) | Manual photoresist coating | prebake (HP 90C, 60”) | Exposure (L05C) |
| --- | --- | --- | --- |
| P.E.B. (HP 120C, 90”) | Development (manual) (LOR 45”, others 70”) | H.B. (HP 120C, 60”) |  |

- For manual coating and development--contact Engineer Hung-Chun Chen at ext. 7575.

- A breakage of size 12*12, 20*20 or 25*25mm2 can be coated and developed automatically in L09--contact Engineer Chao-Hsin Hung at ext. 7573.

Requirements on use of breakage lines – (3)

Exposure requirements:

- Only those who are qualified to use breakage lines are permitted to use jigs.

- Jigs are provided by the engineer; do not take them out of the cabinet yourself.

- All jigs must be used carefully.

- The exposure jigs have been patented. Do not take their pictures for imitation, or you will violate intellectual property rights.

- Be careful when wiping the slides, and return them to their original positions after wiping.

- Please return everything to its original position after an exposure is completed.

- Please keep the working table clean, and do not leave any wipes or vacuum tape on the table. Violation of the foregoing will be subject to penalty.