I-line Breakage Line-Standard Process

Chin-Tsai Hsu

Jan. 9, 2020

I-line Breakage Line-Process Specifications--(1)

Thickness of breakage: must be725 um

Type: may be Si, compound semiconductors, glass, and LiTaO3 ceramic materials

Size: 25*25 mm2 breakage for standard OEM

Reticle, exposure arrangement and size:

Range of reticle layout:

3.2 X 3.2mm2 (for 9 IN 1 reticle), 7.2 X 7.2 mm2 (for 4 IN 1 reticle)

Exposure arrangement and size:

5 X 5 map, stepping 4.5 X 4.5 mm2 (for 9 IN 1 reticle), 2 X 2 map, stepping 9 X 9 mm2 (for 4 IN 1 reticle)

Resolution and alignment error:

Resolution: single line 0.35 um/single hole 0.45 um

Alignment error: misalignment 1 um

I-line Breakage Line-Process Specifications--(2)

| 9 IN 1 reticle | 5x5 map (25 mm2) 3.2x3.2 mm2 exposure area Stepping 4.5x4.5 mm2 |  | 4 IN 1 reticle |  | 2x2 map (25 mm2) 7.2x7.2 mm2 exposure area Stepping 9x9 mm2 |
| --- | --- | --- | --- | --- | --- |
| Minimum resolution: single line 0.35 um single hole 0.45 um |  | Reserve at least 1 um for the design of layout alignment error |  |  |  |  |