Notes on OEM for Breakage Lines of L05C I-line Stepper

Revision date: Jan. 9, 2020

- Standard size for breakage line OEM: 2.5cm*2.5cm; for non-standard size, contact our engineers for service.

- Thickness of breakage: must be less than 725 um.

- A 5x7 cm2 dummy breakage is required (dummy breakage is not required for 6- or 8-inch cut breakage).

- For breakages that require multi-layer alignment under the OEM service, use the cutting machine to cut them; otherwise it cannot be guaranteed that OEM service for multi-layer alignment will be available.

- Time for breakage OEM: Every Tuesday/Thursday from 14:00 to 16:00. No more than 4 breakages will be accepted per service. Any service for more than 4 breakages must be requested with 2 forms. Exposure will be scheduled according to the number of the application form.

- The photoresist coating and development for breakage must be performed by the user (for automatic coating and development, contact Engineer Chao-Hsin Hung via 7573; for manual coating and development, contact Engineer Hung-Chun Chen via 7575).

- For breakage, perform zero-layer exposure and etching (with an etching depth of more than 200 nm) first. Please memorize the file name and content of an exposure for breakage OEM.

- Only single-layer exposure is required; zero-layer exposure is not necessary. The size of a breakage can be unlimited, but must be subject to a discussion with the engineer first.

- The reticle for breakage OEM is: 9-in-1 reticle or 4-in-1 reticle -- for reticle layout and production, contact Ying-Ling Hong via 7746.

- The minimum resolution for breakage OEM is 0.4 um L/S, 0.35 um single line and 0.45 um hole pattern, and misalignment spec ≤ 1 um. If you have any other special requirements, contact the engineer for discussion.

- The fee for breakage OEM is charged per breakage: 10 pieces per breakage.

Example: For 4 breakages requested by the academia, the actual fee paid = (NT$250/piece)*(10 pieces/breakage)*(4 breakages)*10% = NT$1000

I-line engineer Chin-Tsai Hsu ext.: 7648 (cthsu@narlabs.org.tw)