Introduction of Focused Electron Beam System

Instrument no.: L18

Instrument name: Focused Electron Beam System

Storage location: Class 10 Photo Room

Model: FEI Helios 1200+

The functions are described as follows:

This instrument features three main functions:

- It utilizes the excellent resolving power of electron beam for electron beam induced deposition of platinum or carbon, and traces patterns to produce hard masks for subsequent resistance to etching. It can create a nano-structured aligner for prototyping.

- Its gun, combined with an ion beam, can be used to cut a section directly on the sample and observe the section with an electron beam, making it a good tool for failure analysis.

- The high-voltage ion beam can cut sections on both sides to make a TEM sample and, combined with the low-voltage ion beam technology for sample cleaning, can produce an excellent TEM sample smaller than 100nm with low-amorphization damage.

The main specifications are described as follows:

| Electron beam specifications |  |
| --- | --- |
| Resolving power | 1nm @ 15kV SE 1.4nm @ 1kV SE |
| Accelerating voltage | (SEM) 1-30kV |
| Electron emission source | Thermal field emission |
| Range of magnification for observation | (SEM) 55x to 500kx |
| Ion beam specifications |  |
| Resolving power | 4.0nm achievable@30kV |
| Accelerating voltage | (FIB) 2-30 kV |
| Ion emission source | Type: Gallium liquid metal Life time: 1000 hours |
| Stability of position of ion beam irradiation | Beam shift spec.: mechanically <5μm, electrically 0.1% |
| Specifications of movable stage |  |
| Direction axis | At least 5-axis motorized |
| Specifications of movement X, Y | Repeatability 2.5 μm Travel ≥± 200 mm |
| Z | ≥ 10mm |
| Rotation | 360° |
| Tilt | -3° to 58° |
| Sample stage | 200-300 mm wafer |
| Applicable gases | Platinum Deposition Carbon Deposition |