Variable Shaped Electron Beam Aligner Standard Process

NEB resist process sequence

aim: ~380nm resist thickness

| - Prime | HMDS 90°C |
| --- | --- |
| - Coating | 4400 rpm 30” |
| - Softbake | 110°C 120” |
| - Exposure | Base Dose 16µC/cm2 |
| - Post Exposure Bake | 105°C 120” |
| - Development | AD-10 2.38% TMAH 60” puddle |
| - Rinse | Di-Water |
| - Hardbake | 110°C 120” |

  - Track ACT8 recipe

- COT-NEB

- DEV-NEB

| 100 nm line 101.3 nm iso @12µC/cm2 | 101.7 nm L/S=1:3 @11.2µC/cm2 |
| --- | --- |
|  | Collapse L/S=1:1 @12µC/cm2 |

CAN resist process sequence

aim: ~100nm resist thickness

| - Prime | HMDS 90°C |
| --- | --- |
| - Coating | 1500 rpm 30” |
| - Softbake | 110°C 90” |
| - Exposure | Base Dose 80µC/cm2 |
| - Post Exposure Bake | 110°C 60” |
| - Development | AD-10 2.38% TMAH 30” puddle |
| - Rinse | Di-Water |
| - Hardbake | 110°C 60” |

  - Track ACT8 recipe

- COT-CAN

- DEV-CAN

| 50 nm line 47.9 nm iso @80µC/cm2 | 49.5 nm L/S=1:3 @76µC/cm2 |
| --- | --- |
|  | 48.5 nm L/S=1:1 @72µC/cm2 |

Chips placement on 8” wafer (standard layout)

Chip mark arrangement in the chip