| Programs for 5-inch reticle (Do not run the program until the temperature of the “thermostat” in the power box reaches the set value) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process No. Program No. | Name | Work Select Reticle Specification | Description | Step 1 | Step 2 | Step 3 | Step 4 | Step 5 |
| 11 | 5"_FEP-171_COT | 5inch : t23 (5009) | Resist1: FEP-171(3mPa.s) coating | Coater 20 | HP1 130 °C/350 sec |  |  |  |
| 12 | 5"_NEB22-A2_COT | 5inch : t23 (5009) | Resist2: NEB22-A2(2mPa.s) coating | Coater 19 | HP2 120 °C/390 sec |  |  |  |
| 13 | 5"_FEP-171_DEV | 5inch : t23 (5009) | Resist1: FEP-171(3mPa.s) development | HP2 120 °C/360 sec | CP 23 °C/300 sec | Develop 10 | HP2 120 °C/450 sec |  |
| 14 | 5"_NEB22-A2_DEV | 5inch : t23 (5009) | Resist2: NEB22-A2(2mPa.s) development | HP1 115 °C/420 sec | CP 23 °C/300 sec | Develop 10 | HP2 120 °C/450 sec |  |
| 08 | 5"HB | 5inch : t23 (5009) | HB Hard bake | HP2 120 °C/450 sec |  |  |  |  |
| 04 |  |  |  |  |  |  |  |  |
| 05 |  |  |  |  |  |  |  |  |

| Programs for 6-inch reticle (Do not run the program until the temperature of the “thermostat” in the power box reaches the set value) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process No. Program No. | Name | Work Select Reticle Specification | Description | Step 1 | Step 2 | Step 3 | Step 4 | Step 5 |
| 16 | 6"_FEP-171_COT | 6inch : t6.35 (6025) | Resist1: FEP-171(3mPa.s) coating | Coater 17 | HP1 140 °C/420 sec |  |  |  |
| 17 | 6"_NEB22-A2_COT | 6inch : t6.35 (6025) | Resist2: NEB22-A2(2mPa.s) coating | Coater 18 | HP2 130 °C/420 sec |  |  |  |
| 18 | 6"_NEB22-A2_DEV | 6inch : t6.35 (6025) | Resist2: NEB22-A2(2mPa.s) development | HP1 125 °C/420 sec | CP 23 °C/300 sec | Develop 11 | HP2 130 °C/510 sec |  |
| 19 | 6"_FEP-171_DEV | 6inch : t6.35 (6025) | Resist1: FEP-171(3mPa.s) development | HP2 130 °C/420 sec | CP 23 °C/300 sec | Develop 11 | HP2 130 °C/510 sec |  |
| 09 | 6"HB | 6inch : t6.35 (6025) | HB Hard bake | HP2 130 °C/510 sec |  |  |  |  |
| 06 |  |  |  |  |  |  |  |  |
| 07 |  |  |  |  |  |  |  |  |