L22 High-speed Mass-produced Optical Exposure System

Technical Data

(248 Scanner Technology Data)

Responsible engineer: Tsai-Ming Huang

Engineer: Tsai-Ming Huang

Last Edit: Aug. 16, 2022

GKR-5201A Resolution

- Substrate: Double-side polished silicon wafer

- Photoresist: GKR-5201A (3160Å)

- Reticle: Binary Mask

- Line width design Line/Space: 110/110 nm

| Location | Linewidth (nm) |
| --- | --- |
| Center | 109.6 |
| Left | 108.3 |
| Right | 108.5 |
| Up | 109.5 |
| Down | 109.7 |

TDUR-P6159 Resolution

- Substrate: Double-side polished silicon wafer

- Photoresist: TDUR-P6159 (8000Å/20000Å)

- Reticle: Binary Mask

| 248 | P6159 |  |  |
| --- | --- | --- | --- |
| PR Thickness (A) | 8000 |  | 20000 |
| Resolution | Line/Space: 0.25 um | Hole/Pillar: 0.35 um | Line/Space: 0.8 um Dense Hole/Pillar: 1 um |

L/S

Hole

Pillar

L/S

Pillar