Introduction of 4-point Metal Probe

- Hardware:

- 4-point probe measurement system

- Controlling computer

- Usage: Measurement of the resistance of metal film, and inspection of the uniformity of metal film.

- Description of functions

Automatic measurement: single-point, 3-point or 5-point measurement and wafer mapping.

Manual measurement: Adjustable number of points and range of measurement (applicable for breakages).

- Measurement range: 0.5 m - 400 M Ω∕square

- Substrate size: > 1cm x 1cm

- Update: August 10, 2005