Standard Process for Metal Four-point Probe

- The chip size must not exceed 6 inches; breakage is acceptable.

- Automatic and manual measurement of multiple points.

- Measurement range:  0.5 m to 400 M Ω∕square.

- The metal film is preferably deposited on SiO2 or a silicon chip of the insulation layer to maintain measurement accuracy.

- Substrate size: > 1cm x 1cm

- The function of wafer mapping can be used to check the uniformity of the deposited metal (as shown in the figure below).