Notes on Metal Four-point Probe

- Measurement range:  0.5 m to 400 M Ω∕square.

- Before measurement, please turn on the pump switch underneath and make sure the chip is attached to the measuring stage.

- Please write down the measurement data of the machine on a sheet of paper. The functions of printing and network connection are not available for the machine.

- Note: the specimen size must exceed 1cm x 1cm.

- Silicon wafers are the main substrate for metal films. For other materials, please contact the engineer.

- Metal films are preferably deposited on SiO2 or other insulation materials to obtain more accurate data.