Standard Process for N&K

- Substrate: Si wafer

- Substrate size: > 5cm x 5cm

- Measure thickness and N value for single layer or multiple layers

- N, K database contains: III-V compounds ; Ge compounds ; Glasses ; Nirtrides; Oxides; Oxynitrides; Silicides; Si; Si compounds.