Introduction of Horizontal furnace system

| Machine No. | System name | Open Level | Location |
| --- | --- | --- | --- |
| CF-T03 | Horizontal Furnace | B2 | Nano/ Class 100 |

- Spec and model of Horizontal furnace system:

- SVCS Furnace system (including oxidation, diffusion and low pressure chemical vapor deposition system) for 6" or 4" wafers (round).

- Allows up to 22 wafers in a single run (control wafer and front/end dummy wafers excluded).

- Standard process:

| Process |  | Temperature (°C) | Specifications |
| --- | --- | --- | --- |
| Tube 01 | Poly-Si/α-Si (LPCVD) | 620/560 | 200~10,000Å |
| Tube 02 | Nitride (LPCVD) | 780 | 30~10,000Å |
| Tube 03 | TEOS-Oxide (LPCVD) | 700 | 30~10,000Å |
| Tube 04 | Dope-AMM (LPCVD) | 560 | 200~10,000Å |
| Tube 05 | Wet-Oxidation Dry-Oxidation | 980/1100 800/900 | 300~10,000Å 30~800Å |
| Tube 06 | Drive-In/N+ Anneal | 400~1,100 | 30 minutes~48 hours |
| Tube 07 | P+ Anneal | 600~950 | 30 minutes~48 hours |
| Tube 08 | H2 Sinter | 300~700 | 10 minutes~2 hours (5%H2/N2) 10 minutes~48 hours (N2) |

- Special notes:

- Fill in the chip form, material, type and concentration of impurities, orientation, thickness, diameter, shape and quantity of the commissioned chip.

- Except new wafers, please state what NDL process the wafer has gone through previously. (e.g.: is the wafer covered with photoresists?).

- No wafers with cracks, photoresist, metal, unknown objects or III-V materials are allowed. No wafers processed by non-NDL front-end equipment are allowed.

- Nitride has a high force and the lab is not liable for wafer cracks, scratches or acicular matter (please take this risk into consideration prior to application).

- For users violating the aforementioned regulations and thus leading to machine contamination or damage, rights of use will be suspended and the user will be held responsible for compensation.