# Introduction of Vertical furnace system

| Machine No. | System name/Class 100 | Open Level | Location |
| --- | --- | --- | --- |
| CF-T13 | Vertical Furnace | B3 | Nano Class 100 |

- Spec and model of Vertical furnace system:

- ASM Vertical Furnace system, for 8” wafer.

- Up to 100 wafers in a single run.

- Standard process:

| Process |  | Temperature (°C) | Specifications |
| --- | --- | --- | --- |
| Tube 01 | Dry-Oxidation | 800 900 | 20~100Å 100~500Å |
|  | Wet-Oxidation | 900 1000 | 200~1,000Å 1000~5,000Å |
| Tube 02 | N+ Poly-Si | 550 | 100~5,500Å |
|  | Poly-Si | 623 | 100~5,000Å |
|  | α-Si | 550 | 100~1,000Å |

- Special notes:

- Fill in the chip form, material, type and concentration of impurities, orientation, thickness, diameter, shape and quantity of the commissioned chip.

- Except new wafers, please state what TSRI process has this wafer gone through previously. (e.g.: is the wafer covered with photoresists?).

- No wafers with cracks, photoresist, metal, unknown objects or III-V materials are allowed. No wafers processed by non-NDL front-end equipment are allowed.

- The acceptable thickness is up to 10,000Å.

- For users violating the aforementioned regulations leading to machine contamination or damage, rights of use will be suspended and the user will be held responsible for compensation.