Introduction of 8” front-end plasma enhanced chemical vapor deposition system

(Front-end PECVD)

Deposit SiH4-based SiOx film and

SiH4-based SiNx films on up to 8” wafers. System features include:

Deposition rate:

SiOx deposition rate > 400 nm/min.

SiNx deposition rate > 150 nm/min.

U% inspection: SiOx/SiNx < 5 %.

Dielectric constant: must be between 3.9~4.2 for SiOx.

must be between 7.0~9.0 for SiNx.

Refractive index: SiOx film @635nm 1.465 +/- 0.015.

SiNx film @635nm 2.02 +/- 0.03.

Metal elements under 50E10 atoms/cm2, like Fe, Cr, Ni, Cu, Zn and Co.