Introduction of T29-Physical vapor deposition (PVD) system

- System introduction

- System name: Physical vapor deposition (PVD) system

- Manufacturer: ULVAC, Inc.

- Mode: ENTRON W200 1E2T2L 200mm dia. wafer

- System functions: Metal film, metal oxide and nitride film deposition

- System structure: (refer to Figure below)

  - Load lock Chamber: LA, LB

  - Transfer Chamberl: FX, RX

  - ICP Chamberl: F1

  - Process Chamber: F3, R1, R2

- Function introduction

System functions:

- ICP Chamber F1: Remove SiOx on chip surface

- Process Chamber F3: (ternary target chamber) Al/Si/Cu, Ti, TiN, TiOx, Ni, NiOx

- Process Chamber R1: Ti, TiN, Ni

- Process Chamber R2: Al/Si/Cu, Al/Cu

- System restrictions

- No broken wafer allowed

- Only 8” wafers allowed

R1 R2 F2 Triple-Gun LA LB FX RX F1

Fig. 1. System structure