Uniform metal film deposition system (T29)

- Current standard processes

  - Al/Cu or Al/Si/Cu

(Max. thickness is 3000 Å. Thickness > 1000 Å will be achieved by multiple depositions in the chamber)

    - 500Å

    - 800 Å

    - 1000 Å

    - 1500 Å

  - TiN

(Max. thickness is 3000 Å. Thickness exceeding 500 Å will be achieved by multiple depositions in the chamber)

    - 100Å

    - 200 Å

    - 400 Å

    - 500 Å

  - Ni

(Max. thickness is 1000 Å. Thickness > 500 Å will be achieved by multiple depositions in the chamber. )

A non-recurring device for Ni target is available in the chamber. Please confirm the target type in the chamber before Ni plating process.

    - 100 Å

    - 150 Å