# Introduction of Ultra high metal and metal oxide nano-level film sputtering system

# System introduction

  - System name: Ultra high vacuum metal and metal oxide nano-level film sputtering system

  - Manufacturer: Applied Materials, Inc.

  - Model: Endura® Clover™ MRAM PVD System

  - System function: Metal and metal oxide nano-level film deposition

  - System structure: (refer to Figure below)

    - Loadlock Chamber: LLA, LLB

    - Transfer Chamber: Transfer, Buffer, Ch.A, Ch.B

    - Deposition Chamber: Ch.2, Ch.3, Ch.5

    - Degas Chamber: Ch.F

    - Cryo-cooling Chamber: Ch.B

    - Oxidation Chamber: Ch.1

# Function introduction

System functions:

  - Degas Chamber F: Degassing, thermal annealing

  - Deposition Chamber 2: (Quinary target chamber) CoFeB25, CoFeB20, CoFe, Mo, Mg

  - Deposition Chamber 5: (Quinary target chamber): Co, Pt, Ru, Ta, W

  - Deposition Chamber 3: MgO

  - Cryo-cooling Chamber B: Cooling after MgO barrier deposition

  - Chamber A: Ar cooling

  - Oxidation Chamber 1: Mg oxidation

# System restrictions

  - Silicon substrates

  - The growth surface must be Si, Ge, SiOx and stable solid-state metals

  - No broken wafer allowed

  - Only 8” and 12” wafers allowed

  - No photoresist allowed

Fig. 1. System structure