Ultra-high metal and metal oxide nano-level film sputtering system

- Thin films that can be deposited by current standard processes: Co, Pt, Ru, Ta, W, CoFeB25, CoFeB20, CoFe, Mo, Mg and MgO; thickness limit of each layer: 3 Å~200 Å