Introduction of Metal organic chemical vapor deposition (MOCVD) (Veeco Propel 200)

- Key features:

This metal organic chemical vapor deposition (MOCVD), equipped with front-end chambers for growing epitaxy in high temperatures, is a system for 2DEG structure of GaN. Epitaxial growth through high-temperature, high-speed wafer rotation and vertical gas flow incorporates epitaxy source TMGa and TMA1 as well as reactive gas NH3 to realize high-quality/low-defect epitaxy that cannot be achieved by nitrides grown in low temperatures. Main epitaxial structure is a High electron mobility transistor (HEMT structure). The film thickness can be controlled between 2nm~5000nm. During epitaxial growth, an in-situ optical monitor and real-time interference monitoring on film growth are utilized to accurately control wafer warpage resulting from thermal stress and to calculate the bow value.

# Epitaxial materials:

  - Nitride epitaxial layers such as GaN, AlGaN, AlN, etc.

  - E-mode / D-mode HEMT epitaxy.

# MOCVD machine ID card

- Full name: 	Metal organic chemical vapor deposition (MOCVD) system

- Location: Experiment Building / class 1000

- Engineer: 	Long-Xing Xu (O) ext.: 7587 (C)

- Substitute: 	Long-Xing Xu (O) ext.: 7587 (C)

- Person-in-charge:   Long-Xing Xu (O) ext.: 7587 (H)

- Chemicals in work area:

  - Bulk gases: N2, H2

  - Specialty gases: No

  - Bottled chemicals:

    - Organic compounds:

    - Acid/alkali:

    - Oxide:

    - Others:

- Process mode or reaction chamber:

(1)

(2)

- Reaction chamber vacuum range:10 torr (Process: 10~200 torr)

- Vacuum pump: 	Turbo pump, Dry pump

- Substances in exhaust emissions: H2, N2

- Type of exhaust extraction pump: Dry pump

- Separate local scrubber: Yes

- Reaction chamber temperature range: 500°C - 1100°C

- Type of cooling system: Chiller, cooling wafer supplied by facility

- Manufacturer/agent:  Veeco Taiwan