Test Report

Test Report No.: T-NM-002-110-001

| Customer Profile |  |  |  |
| --- | --- | --- | --- |
| Name | Taiwan Semiconductor Research Institute | Customer | Nien-Chih Lin |
| Tel.: | 03-5773693#7709 | E-mail | 1805034@narlabs.org.tw |
| Address | No. 26, Prosperity Road I, East Dist., Hsinchu City |  |  |

| Test Profile |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Order No.: S-110-TAF-004 | Test Name: Step Height Measurement |  |  |  | Test Item Qty.: 1 |
| Test Instrument Model: NM-002, Veeco D5000 |  |  | Measurement Location: R221 |  |  |
| Commission Date: 08/24/2021 |  | Analysis Date: 08/25/2021 |  | Completion Date: 08/25/2021 |  |
| Test Item No. and Description: Measuring the step height of the surface structure. |  |  |  |  |  |
| Test Method: |  |  |  |  |  |
| The test was performed in accordance with the N3-TM01 Standard Operating Procedure for Atomic Force Microscopy for Large Specimens Ver. 1.0. |  |  |  |  |  |
| Test Specifications: |  |  |  |  |  |
| Reference standard: VLSI 6429-004-049; Scan mode: Tapping mode. Tip: NANOSENSORS PPP-RT-NCHR; Scan size: 5um. Environmental conditions; Scan rate: 0.5Hz. Temperature: 25.3°C, Humidity: 51.7%. |
| Test Result: No.; S-110-TAF-004-a. Customer’s Test Item No.; F1. Measured Line Spacing Value (nm); 424. |

| Test Engineer |  | Report Signatory | Technical Manager |
| --- | --- | --- | --- |
| Quality Manager |  | Laboratory Manager | Laboratory Seal |
| Note: | - This report shall not be extracted or copied, except in its entirety, without the written consent of the Laboratory. - The test item used in this report was provided by the customer. The Laboratory is liable only for the test result of the test item. - This report is valid only with the seal and signature of the Laboratory. - The information shown in this report is used for reference only and shall not be used for other purposes such as commercial advertisement or evidence in legal proceeding. |  |  |

| No. | S-110-TAF-004-a |  | Customer’s Test Item No. | F1 | Measured Value | 424 nm |
| --- | --- | --- | --- | --- | --- | --- |

２２