Manual Spin Coater

Standard Operation Procedures

- Turn on the Pump before use (press the [Power] button), select the appropriate

suction head (chuck), confirm that the wafer can be sucked , set step1 (low) and

step2 (high) speed value (RPM) and time (seconds), press the red start button on

the right, and turn off the Pump after use (press the [Power] key).

2. Please heat the Hot Plate before use. Please turn it off if you don’t use it for more

than 1 hour to prolong the life of the heating plate. Do not exceed the upper limit of

the operating temperature of 200 degrees. When not in use, you need to pull out

the plug.

3. When using a spin coater, in order to avoid contamination and organic liquids

flowing into the cavity, it is necessary to lay a dust-free wipe in the spin coater and

clean it after use.

4. Please clean up after use, put the used utensils back in place, and close the door of

the fume hood.

5. During use, please try to pull down the door of the fume hood so that the operation

is not affected, so as to reduce the solvent volatilization into the stagnation-free

room.

Start

Vacuum

Step 1(Low)

Step 2(High)