Taiwan Semiconductor Research Institute

SE-024  Chip To Wafer Bonder

一. System introduction:

1. Equipment name: C2W wafer alignment bonding machine

2. Brand: Finetech

3. Instrument model: Fineplacer sigma

4. Equipment function: Chip to Wafer alignment bonding process

5. Wafer Size: chip size

二. Specifications:

1. A chip-sized heated nozzle head must be customized.

2. Bonding force max 500 N.

3. Temperature max: chip 400 °C & substrate 250 °C.

4. Equipped with Dispenser & Process Video Module.

5. Equipped with Die Flip & Formic Acid Module.