Taiwan Semiconductor Research Institute

SE-025  Wafer To Wafer Bonder

一. System introduction:

1. Equipment name: W2W wafer alignment bonding machine

2. Brand: EVG

3. Instrument model: EVG 501&610

4. Equipment function: Wafer to Wafer alignment bonding process

5. Wafer Size: 6 & 8 inches

二. Specifications:

1. The dry mechanical pump can achieve a vacuum value of about 5E-2 torr.

2. Back alignment objective lens & front IR light source & manual alignment mode.

3. Bonding force max 20kN.

4. Max temperature can reach 450 °C.

5. Cu-Cu & Sn-Sn & Glass Carrier Bonding.